## Slide 1
Non-Credit Graduate Course:
The Thermochemistry of Smouldering Combustion.
by Márcio Ferreira Martins
Seminar II – June 28, 2017

## Slide 2: Seminar III – Kinetics of solid reactions
Step 1. Proximate analysis
Composition (wt.%) | Non-standard (170 K/min)
FC | 4.7
VM | 17.2
Minerals | 34.6
Inert matter | 43.5

## Slide 3: Seminar III – Kinetics of solid reactions
Step 1. Proximate analysis: Strategy

## Slide 4: Seminar III – Kinetics of solid reactions
Step 2. TG/DTG – N2

## Slide 5: Seminar III – Kinetics of solid reactions
Step 2. TG/DTG – Air

## Slide 6: Seminar III – Kinetics of solid reactions
Step 2. TG/DTG – Air x N2

## Slide 7: Seminar III – Kinetics of solid reactions
Step 3. TG/DTG vs. Non-standard
Composition (wt.%) | Non-standard (170 K/min) | TGA (3K/min)
FC | 4.7 | -
VM | 17.2 | 18.0
Carbonates (CaCO3) | 34.6 | 42.3
Inert matter | 43.5 | 39.7

## Slide 8: Seminar III – Kinetics of solid reactions
Step 4. According to the temperature ranges
From pyrolysis:
Water evaporation: 50 - 150 °C
OM → FC + VM: 150–550 °C
Minerals → Minerals + gas: 550–770 °C
IM → IM

## Slide 9: Seminar III – Kinetics of solid reactions
Step 4. According to the temperature ranges
From combustion:
Water evaporation: 50 - 150 °C
OM → FC + VM
FC + O2 : → gas
Minerals → Minerals + gas: 550–770 °C
IM → IM
150–550 °C

## Slide 10: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
From the analysis of weight loss data, the fraction of the material converted,
is weight loss quantity after time “t”,
is total weight loss quantity after a completed reaction.
(1)

## Slide 11: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
From reaction theory, the kinetic equation for decomposition of a solid matter,
order of reaction,
reaction rate constant.
(2)

## Slide 12: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
Assuming an Arrhenius governed problem
Pre-exponential factor
Apparent activation energy
Temperature
Pay attention to the units!
(3)

## Slide 13: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
Combining Eq. (2) and (3) and considering a first-order reaction:
(4)
Non-isothermal analysis
Isothermal analysis

## Slide 14: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
(4)
Non-isothermal analysis
Isothermal analysis
Direct Arrhenius plot method
Differential method of Friedman
Integral methods of Ozawa.
…
Model-fitting approach

## Slide 15: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
Direct Arrhenius plot method:
Considering , Eq. (4) becomes:
(5)

## Slide 16: Seminar III – Kinetics of solid reactions
Step 5. Mathematic models
Direct Arrhenius plot method:
Taking the logarithm of both sides of Eq. (5)
(6)

## Slide 17: Seminar III – Kinetics of solid reactions
Step 6. Direct Arrhenius plot method